## Slide 1: Синхротронні дослідження квантових матеріалів
Олександр Кордюк
Київський академічний університет
kordyuk@gmail.com

## Slide 2
Kyiv Academic University
Department of Applied Physics and Nanomaterials > https://kau.org.ua/en/kordyuk
G.V. Kurdyumov Institute for Metal Physics of NAS of Ukraine
Department of Superconductivity > https://www.imp.kiev.ua/~kord
Leibniz Institute for Solid State and Materials Research Dresden - IFW Dresden
Leibniz Lab in Kyiv > https://gu-qumat.ifw-dresden.de
German-Ukrainian Center for Quantum Materials https://kau.org.ua/gu-qumat
Eastern European Synchrotron Light Source in Ukraine
https://vuias.org
National Research Foundation of Ukraine https://nrfu.org.ua

## Slide 3
Навчання через передові дослідженнях передові = цікаві
Міжнародна співпраця
Студенти та молоді науковці
Дослідницька інфраструктура
Мета КАУ: залучення студентів до наукових досліджень через синергію освіти, науки та інновацій
Квантові матеріали + квантові технології
Машинне навчання для досліджень: конденсована речовина, астрофізика, біологія, математика
Розвиток дослідницької інфраструктури (синхротронні дослідження)

## Slide 4: UKRATOP – a research+ bilateral project on Topological Quantum Materials
Scholarships: 21 MSc students; 2 PhD students; 5 PostDocs.
Experience in highest level research
and communication, strengthening p2p collaboration
All MSc and PhD students defended their degrees in Ukraine
Exp. equipment from IFW Dresden installed in Kyiv
https://kau.org.ua/ukratop
KAU+IFW & TU Dresden: 1 000 000 EUR, 2018-2024

## Slide 5
Scientific Output
2024
Nature 626, 294 (2024)
2023
J. Cryst. Growth 619, 127332 (2023)
Phys. Rev. B 107, 165141 (2023)
Phys. Rev. Materials 7, 033405 (2023)
Phys. Rev. B 107, 035158 (2023)
Phys. Rev. Materials 7, 014003 (2023)
Phys. Rev. Materials 7, 014003 (2023)
2022
Phys. Rev. B 106, 085401 (2022)
Phys. Rev. Lett. 129, 227203 (2022)
Phys. Rev. B 106, 174426 (2022)
J. Phys. D. Appl. Phys. 55, 445003 (2022)
J. Solid State Chem. 314, 123416 (2022)
Nature Comm. 13, 4132 (2022)
Crystals 12, 998 (2022)
Phys. Rev. B 105, 235112 (2022)
Phys. Rev. Lett. 128, 036402 (2022)
Phys. Rev. B. 105, 024410 (2022)
Comput. Mater. Sci. 203, 111089 (2022)
Small 18, 2105219 (2022)
2021
Phys. Rev. Lett. 127, 045701 (2021)
SciPost Phys. 10, 004 (2021)
Dalton Transactions 51, 361 (2021)
Crystals 11,500 (2021)
Cryst. Growth Des. 21, 3063(2021)
J. Cryst. Growth 562, 126082 (2021)
J. Alloys Compds. 855, 157334 (2021)
Ukr. J. Phys. 66, 333 (2021)
2020
SciPost Phys. 9, 043 (2020)
Nano Lett. 2020, 20, 11, 8157 (2020)
Appl. Phys. Lett. 116, 222406 (2020)
Phys. Rev. Materials 4, 124202 (2020)
npj Quantum Materials 5, 67 (2020)
Phys. Rev. B 102, 220408(R) (2020)
npj Quantum Materials 5, 22 (2020)
2019
SciPost Phys. 7, 035 (2019)
Phys. Rev. B 99, 014404 (2019)
Phys. Rev. B 99, 184429 (2019)
Phys. Rev. B 100, 140407(R) (2019)
Mater. Res. Express 6, 106319 (2019)
APL Materials 7, 121106 (2019)
Low Temperature Physics 45, 1172 (2019)
UKRATOP
S. Borisenko et al.
Fermi surface tomography.
https://kau.org.ua/ukratop
Evidence of superconducting Fermi arcs A. Kuibarov, A. Suvorov, et al.
Notes: There are many results, and among the latest is the Nature paper of KAU and UKRATOP alumni about new topological superconductors PtBi2.

## Slide 6
German-Ukrainian Center for Quantum Materials
Німецько-український центр квантових матеріалів
Синтез нових матеріалів
Вирощування монокристалів (оптичні печі в Києві та Дрездені)
Створення плівкових гетероструктур (система високовакуумного магнетронного напорошення, Київ)
aiming in the theory assisted search for new quantum materials
Notes: Another result is the new GU-QuMat project that aims in Theory-assisted search for new quantum materials’.

## Slide 7
German-Ukrainian Center for Quantum Materials
Німецько-український центр квантових матеріалів
Експериментальні дослідження квантових матеріалів
розвиток експериментальної інфраструктури в Києві
синхротронні дослідження електронної структури
aiming in the theory assisted search for new quantum materials
Notes: Another result is the new GU-QuMat project that aims in Theory-assisted search for new quantum materials’.

## Slide 8
MAVKA – проєкт побудови українського бімлайна на синхротроні SOLARIS

## Slide 9: Accelerator based light sources: Synchrotrons
To watch:
Herman Winick (SLAC) - Public Lecture—Synchrotron Radiation: The Light Fantastic https://youtu.be/N24iTlPvAxY
David Attwood. Introduction to synchrotron radiation https://youtu.be/_DWDZzsZL3w https://player.slideplayer.com/15/4610895/#
What are SYNCHROTRONs? SLAC National Accelerator Laboratory https://youtu.be/g6OZmKb_tIU
Diamond Light Source: Synchrotron technology https://youtu.be/_xv_GwCgpAc | Virtually Visit https://www.diamond.ac.uk/Public/VisitUs/Virtual-Visit.html
Elettra. What is a synchrotron? How does it work? https://youtu.be/l4NSF-gkKCU
Tour of MAX IV accelerators with professor Sverker Werin https://youtu.be/2TJMFlkyFwc
SOLARIS synchrotron - How does it work? https://youtu.be/McPodwqR5ww
ESRF, the European Synchrotron https://youtu.be/3fEIS6pbhIo | ESRF-EBS, a revolutionary new synchrotron https://youtu.be/tCwJ_CB2cyM
24 hours in a synchrotron. nature video https://youtu.be/UsJ1j4_1Di0

## Slide 10
What Is a Synchrotron?
Historical Background: Early experiments, discovery of synchrotron radiation, and key developmental milestones.
Global Landscape: Major synchrotron facilities worldwide and their unique features; LEAPS.
Construction & Principles of Operation: How synchrotrons accelerate particles, produce intense X-rays, and the main components (e.g., injector, storage ring, beamlines).

## Slide 11
3.5 TeV per beam in 2010 and 2011
4 TeV in 2012 upgrades to 6.5 TeV mid-March 2015
27 km in circumference, 175 m deep
1998 – 2008
7.5 billion euros (approx. $9bn)
Large Hadron Collider (LHC)
protons travel at 99.999999988% the speed of light
Notes: 11
У Великому адронному колайдері використовується 10 000 надпровідних магнітів та 1200 тон надпровідного кабелю з NbTi. Обмеження у енергії адронів визначається критичним магнітним полем.

## Slide 12: Stanford Linear Accelerator Center -> SLAC National Accelerator Laboratory
https://www6.slac.stanford.edu
Herman Winick (SLAC) - Public Lecture— Synchrotron Radiation: The Light Fantastic https://youtu.be/N24iTlPvAxY
How did Synchrotrons become global X-ray powerhouses? https://youtu.be/Cv1oaI2CcBk
1966 - Construction completed
1973-1977 - Stanford Synchrotron Radiation Project
2002-2009 - Linac Coherent Light Source project
2023 - LCLS-II produces first light

## Slide 13
https://www6.slac.stanford.edu
How did Synchrotrons become global X-ray powerhouses? https://youtu.be/Cv1oaI2CcBk

## Slide 15: Stanford Linear Accelerator Center -> SLAC National Accelerator Laboratory
https://www6.slac.stanford.edu
SSRL utilizes x-rays produced by its accelerator, the Stanford Positron Electron Asymmetric Ring (SPEAR3)
Stanford Synchrotron Radiation Lightsource (SSRL)

## Slide 16
What Is a Synchrotron?
Historical Background: Early experiments, discovery of synchrotron radiation, and key developmental milestones.
Global Landscape: Major synchrotron facilities worldwide and their unique features; LEAPS.
Construction & Principles of Operation: How synchrotrons accelerate particles, produce intense X-rays, and the main components (e.g., injector, storage ring, beamlines).

## Slide 17
> 50 synchrotrons light sources around the world
Materials Today Physics (2018) https://doi.org/10.1016/j.mtphys.2018.09.002

## Slide 18: League of European Accelerator based-Photon Sources
https://www.leaps-initiative.eu
LEAPS unites all Synchrotron and Free Electron Laser accelerators in Europe: 19 facilities involving over 30,000 scientists from 93 countries.
It was created in 2017 with the primary goal of actively and constructively promote and ensure the quality and impact of fundamental, applied and industrial research carried out at its members.
2024 LEAPS Brochure
https://www.leaps-initiative.eu/resources/

## Slide 19
https://youtu.be/tCwJ_CB2cyM
https://youtu.be/6EHqtsF6Vrw

## Slide 20
BESSY
https://www.helmholtz-berlin.de/en/about-us/

## Slide 21
BESSY @ Berlin Adlershof

## Slide 26
Elettra Sincrotrone Trieste
https://www.elettra.eu/

## Slide 29
What Is a Synchrotron?
Historical Background: Early experiments, discovery of synchrotron radiation, and key developmental milestones.
Global Landscape: Major synchrotron facilities worldwide and their unique features; LEAPS.
Construction & Principles of Operation: How synchrotrons accelerate particles, produce intense X-rays, and the main components (e.g., injector, storage ring, beamlines).

## Slide 30
Synchrotron
LinAc
Storage Ring
Booster
Beamlines
Andulator
Bending magnets
Notes: Both anomalous in 2D.

## Slide 34
https://youtu.be/aXRTczANuIs

## Slide 35: Electromagnetic radiation spectrum
Source: Lawrence Berkeley National Laboratory https://electromagneticworld.blogspot.com/2017/04/electromagnetic-spectrum.html

## Slide 37
https://physics2000.com/PDF/Text/Ch_33_LIGHT_WAVES.pdf

## Slide 38
David Attwood Introduction to synchrotron radiation https://youtu.be/_DWDZzsZL3w
Synchrotron radiation from relativistic electrons
A. Bharti and N. Goyal (2019) https://www.intechopen.com/chapters/65550

## Slide 39
David Attwood Introduction to synchrotron radiation https://youtu.be/_DWDZzsZL3w

## Slide 40
Notes: Both anomalous in 2D.

## Slide 43
Insertion device (undulator)

## Slide 47: ARPES Beamline
Damascelli RMP 2003

## Slide 48
https://www.aig.org.au/australian-synchrotron-visit/

## Slide 54
Facility | Country | Energy [GeV] | Current [mA] | Periphery [m] | Emittance [nm-mrad] | Brilliance [ph/s/mrad2/mm2/0.1%bw]
Spring8 | Japan | 8.00 | 100 | 1436 | 2.80 | 2.0 × 1021
APS | USA | 7.00 | 100 | 1104 | 3.00 | 8.0 × 1019
ESRF | France | 6.00 | 200 | 844 | 3.80 | 8.0 × 1020
Diamond | England | 3.00 | 300 | 562 | 2.70 | 3.0 × 1020
ALBA | Spain | 3.00 | 100 | 268 | 4.58 | 4.0 × 1012
SOLEIL | France | 2.75 | 500 | 354 | 3.70 | 1020
Elletra | Italy | 2.40 | 320 | 260 | 7.00 | 1019
SLS | Switzerland | 2.40 | 400 | 288 | 5.50 | 5.0 × 1015
MAX-IV | Sweden | 2.00 | 500 | 528 | 0.17 | 2.2 × 1021
ALS | USA | 1.90 | 100 | 240 | 6.80 | 3.0 × 1018
BESSY-II | Germany | 1.70 | 100 | 240 | 6.00 | 5.0 × 1018
Main parameters of the synchrotrons
A. Bharti and N. Goyal (2019) https://www.intechopen.com/chapters/65550

## Slide 55
Swiss Light Source (SLS)
2.4 GeV
https://www.psi.ch/en/sls

## Slide 56
Diamond Light Source
https://www.diamond.ac.uk/Home/About.html
3 GeV

## Slide 57
https://www.diamond.ac.uk/Public/VisitUs/Virtual-Visit.html

## Slide 58: Nobel Prizes based on the Utilization of X-Rays
Physics 1901: WILHELM RÖNTGEN 1914: MAX VON LAUE 1915: SIR WILLIAM HENRY BRAGG, SIR WILLIAM LAWRENCE BRAGG 1917: CHARLES BARKLA 1924: KARL MANNE SIEGBAHN 1927: ARTHUR COMPTON 1981: KAI SIEGBAHN
Medicine 1946: HERMANN JOSEPH MULLER 1962: FRANCIS CRICK, JAMES WATSON, MAURICE WILKINS 1979: ALAN M. CORMACK, SIR GODFREY N. HOUNSFIELD
Chemistry 1936: PETER DEBYE 1962: MAX PERUTZ, SIR JOHN KENDREW 1964: DOROTHY HODGKIN 1976: WILLIAM LIPSCOMB 1985: HERBERT HAUPTMAN, JEROME KARLE 1988: JOHANN DEISENHOFER, ROBERT HUBER, HARTMUT MICHEL 1997: PAUL D. BOYER, JOHN E. WALKER 2003: PETER AGRE and RODERICK MACKINNON 2006: ROGER KORNBERG 2009: VENKATRAMAN RAMAKRISHNAN, THOMAS STEITZ, ADA YONATH 2012: ROBERT LEFKOWITZ, BRIAN KOBILKA
Stöhr, J. (2023) In: The Nature of X-Rays and Their Interactions with Matter https://doi.org/10.1007/978-3-031-20744-0_1

## Slide 59
Examples of Cutting-Edge Research
Materials Science & Chemistry: Studying catalysts, superconductors, and advanced materials at atomic-level precision.
Biology & Medicine: Protein crystallography, drug design, and medical imaging.
Art & Archaeology: Non-destructive analysis of artifacts, hidden layers in paintings, and ancient manuscripts.
Defense & Energy: Innovation in armor materials, sensors, battery R&D, and solar cell improvements.

## Slide 60
https://onlinelibrary.wiley.com/doi/10.1002/anie.202404213

## Slide 62
https://physics2000.com/PDF/Text/Ch_33_LIGHT_WAVES.pdf

## Slide 63
https://physikseminar.desy.de/sites2009/site_physikseminar/content/e408/e75/e257234/e257240/e257242/DESY-physics-Chapman.pdf

## Slide 64
Photosynthetic Reaction Center
Discovery: First high-resolution structure of a membrane protein complex central to photosynthesis.
Synchrotron:
  DORIS at DESY (Hamburg, Germany): Instrumental in collecting data for bacterial photosynthetic complexes.
Nobel Prize (Chemistry, 1988): J. Deisenhofer, R. Huber, H. Michel.
https://www.nobelprize.org
Schematic illustration of a reaction centre in a membrane in a photosynthesising bacterium. The figure shows how the photosynthetically active components bacteriochlorophyll (BK), bacteriopheophytin (BF), quinone (Q) and iron (Fe) and the haemgroups of the cytocrome are arranged in the four proteins forming the reaction centre.

## Slide 65
Ribosome Atomic Structure
Discovery: Detailed 3D structure showing how genetic information is translated into proteins.
Synchrotrons:
  DESY (Hamburg, Germany): Early crystallographic data collection by Ada Yonath’s group.
  ESRF (Grenoble, France), APS (Argonne, USA), NSLS (Brookhaven, USA): High-resolution diffraction data for ribosome complexes.
Nobel Prize (Chemistry, 2009): V. Ramakrishnan, T. Steitz, A. Yonath.
https://www.nobelprize.org

## Slide 66
G-Protein–Coupled Receptors (GPCRs)
Discovery: Structures revealing how GPCRs transmit signals across cell membranes.
Synchrotrons:
  APS (Argonne, USA) & ESRF (Grenoble, France): Major facilities for GPCR crystal data collection.
  SSRL (Stanford, USA) & Diamond Light Source (UK): Additional beamlines used in GPCR projects.
Nobel Prize (Chemistry, 2012): R. Lefkowitz, B. Kobilka.
https://www.nobelprize.org

## Slide 67
https://www.elettra.eu/XIIISILS/uploads/Main/Introduction%20to%20Synchrotron%20Radiation.pdf

## Slide 68
https://www.elettra.eu/XIIISILS/uploads/Main/Introduction%20to%20Synchrotron%20Radiation.pdf

## Slide 69
Mechanism of High-Tc Superconductivity: Synchrotron experiments provided direct insight into features such as the pseudogap and spin-charge order, helping refine theories on electron pairing mechanisms.
Topological Insulators: ARPES at synchrotrons confirmed the existence of surface states in materials like Bi₂Se₃, revealing Dirac-like electronic dispersions.
Lithium-Ion Battery Materials: In situ synchrotron X-ray diffraction and X-ray absorption measurements track phase changes and electrode reactions during charging, crucial for improving battery performance.
Perovskite Solar Cells: Synchrotron X-ray scattering elucidates crystal structure and degradation pathways in hybrid perovskites, accelerating advances in next-generation photovoltaics.
Synchrotron Research in Physics and Materials

## Slide 70: Theory assisted search for new quantum materials
Electronic structure is a key.
Combined fast methods for its prediction and measurement.
Machine learning algorithms:
  to help to ’recognise’ the electronic structure of multiband superconductors and the mechanisms (disentangling coherent and incoherent factors) in experimental spectra,
  to calculate their electronic structure,
  and to predict new materials for new applications.
Notes: It is based on the idea that the electronic structure is a key in this search. And we combined fast iterative methods for its prediction in new materials, their synthesis, and measurements.
And machine learning algorithms should play important role here:
- to help to “recognise" the electronic structure of multiband superconductors and the mechanisms (disentangling coherent and incoherent factors) in experimental spectra,
- to calculate their electronic structure,
- and to predict new materials for new applications.

## Slide 71
ARPES: Angle Resolved Photoemission Spectroscopy

## Slide 72
ARPES: Angle Resolved Photoelectron Spectroscopy
Sample
Electron analyzer
ARPES Image
Photons
Fermi's golden rule
Three step model
Notes: 72
І це все дозволяє робити сучасна фотоелектронна спектроскопія з кутовим розділенням (ARPES). Ідейно, метод є дуже простим. Це фотоефект + аналізатор. Електрони, що вибиваються світлом, аналізуються електронним аналізатором. Кут вильоту електронів визначаеться їх імпульсом у кристалі, а аналізатор дає розгортку по енергії, і маємо на вихідному вікні дво-вимірне зображення. Щоб рухати це вікно потрібен маніпулятор що повертає зразок.

## Slide 73: Photoemission spectrum
Electronic structure
A(ω,k)
Electronic excitation spectrum
Probability to find electron with momentum k and energy ω
≡
≡
Electron energy (eV)
Momentum (Å-1)

## Slide 74: Електронна структура під ARPES-мікроскопом: квантуються електронні стани
dk = 2π/L
Імпульс електрона: k
Енергія електрона: ω
Електронна зонна структура: ε(k)
E = mv2/2 = p2/2m
p = ħk
L

## Slide 75
kx
ω
ky
kx
ω
K
Fermi surface
1D
2D
3D

## Slide 76
http://www.phys.ufl.edu/fermisurface/
Nb
Cu

## Slide 77: Structure of electronic spectrum
Electron energy (eV)
Momentum (Å-1)
A(ω,k)
Spectral function
Σ(ω,k) – self-energy
Kordyuk PRB 2005
ε(k) – “bare" electronic band structure
Notes: 77
Два слова про так звані сильно-корельовані системи: цей спектр має свою структуру. Дисперсія голих електронів є скелетом, а розмазка визначається взаємодією електронів, яку називають квазічастинковою власною енергією. Саме шляхом аналізу власної енергії у ВТНП купратах нам вдалося довести магнітний механізм високотемпературної надпровідності.

## Slide 78
L
L
a
Електронна зонна структура: ε(k)
Імпульс електрона: k
Енергія електрона: ω
K = 2π/a
From plane waves to Bloch waves

## Slide 79: The electronic spectrum in the momentum-energy 3D space
kx
ky
EK
TiSe2 – “excitonic insulator”
Kinetik Energy (eV)
Momentum (1/Å)
Notes: 79
От приклад такого розподілу для TiSe2, що є ексітонним ізолятором. Видно багато зон, які можна ідентифікувати та досліджувати.
Тут хочу поділитися ще такою думкою. Більшість курсів з квантової фізики починається зі слів про її складність для розуміння через брак повсякденного досвіду. Так от даний метод дає такі об'єми інформації, що тепер цього сказати буде неможливо.

## Slide 80: Quantum materials
Superconductors
Topological materials
Strogly correlated
CDW/SDW
Semiclassics
Strong correlations
Emergence
Ultra-cold atoms
Cold excitons
Polaritons
Quantum technology
Robert Cava et al. - Introduction: Quantum Materials. Chemical Reviews 121, 2777 (2021)
The rise of quantum materials. Nature Physics 12, 105 (2016)

## Slide 81: Quantum materials
Electron energy (eV)
https://arpes.stanford.edu/research/tool-development/angle-resolved-photoemission-spectroscopy

## Slide 83: The history of superconductivity: the beginning
1911
Hg, TC = 4.2K
Why mercury?
Notes: 83

## Slide 84
1957: BCS
Phonons TC < 25K
Mechanism of superconductivity: BCS
2Δ(0) = 3.5 kTc
kx
ω
Superconducting gap
1972
Notes: 84
Знадобилося 46 років щоб зрозуміти це явище. Так звана теорія БКШ (на честь Бардіна, Купера та Шрифера), пояснювала надпровідність шляхом парування електронів фононами. Важливо, що ця теорія переконала більшість дослідників, що надпровідність вище 25 К є неможливою. Що, звісно, вплинуло на оцінку перспективності практичного застосування надпровідників.

## Slide 85: Experimental proof for the mechanism of superconductivity
metal
insulator
superconductor
V
A
I(V)
dI/dV(V)
Rowell PRL 1963

## Slide 86: High Temperature SuperConductors: Era of Cuprates
Muller & Bednorz
1986
1987
Notes: 86
... високотемпературні надпровідники на основі міді, що були відкриті у 1986 році Беднорцем та Мюлером.
Зважаючи на 25 К ліміт теорії БКШ, це відкриття виявилося вибуховим. Я думаю багато хто пам'ятає той безпрецидентний ажіотаж, який воно викликало. Тоді вважалося, що скоро всі міста стануть надпровідними...
Відомо, що надії на швидкий прогрес у проблемі ВТНП не виправдалися. Насправді, самі дослідження мали багато дуже важливих позитивних наслідків (наприклад, значно стимулювали розвиток експериментальних технік), але:
Загальноприйнятної теорій ВТНП, такої як БКШ, і досі нема. Чи краще сказати, що немає теорії, яка б призвела до створення нових надпровідників з вищими Тс.
Також "не пішли" і багато "очевидних" застосувань ВТНП. Використанню в магнітах, наприклад, заважажє сильно анізотропна густина критичного струму внаслідок якої важко створити потрібну конфігурацію котушки.
Хоча, треба сказати, що погрес у ВТНП дротах за останнє 10-річчя є дуже суттєвим.

## Slide 87
Spin-fluctuations and superconductivity
D. Inosov et al., PRB 2007 T. Dahm et al., Nature Phys 2009
A. Kordyuk et al., EPJ ST 2010
Im G0(k,ω)
Im G(k,ω)
Im χ(q,Ω)
ARPES
INS
ARPES
Розрах.
Formula of cuprates:
Notes: 87
To tell just a little bit more detail about it and highlight the …

## Slide 88
Electronic structure is a key
Band structure is important for Cu-SC
…and in Cu-SC
Multi-band structure is essential for SC in Fe-SC
PRL 92, 257006 (2004); PRB 71, 214513 (2005); PRL 96, 067001 (2006); PRL 96, 117004 (2006); PRL 96, 037003 (2006); PRL 97, 017002 (2006); PRB 75, 172505 (2007); Nature Phys. 5, 217 (2009)...
Nature (2009), PRB (2009)... LTP 38, 888 (2012); JSNM 26, 2837-2841 (2013); PRB 88, 134501 (2013); PRB 89, 064514 (2014), LTP (2018)...
PRL 100, 196402 (2008); PRL 100, 236402 (2008); PRB 79, 020504 (2009); PRL 102, 166402 (2009); PRB 85, 064507 (2012)...
PRL (2018), PRB (2021)

## Slide 89
V. Zabolotnyy Nature 2009
A. A. Kordyuk, J. Supercond. Nov. Magn. 2012
Fermi Surface of BKFA
Notes: The story about IBS also proves the need for both DFT calculations and experiment in order to reveal the true band structure. We see that usually you should shift the band structure +/- 200 meV to fit the experiment.

## Slide 90
"Topological" superconductivity in Fe-SC
LTP 38, 888 (2012); JSNM 26, 2837-2841 (2013); PRB 88, 134501 (2013); PRB 89, 064514 (2014), LTP (2018)...
Notes: And this is crucial to reveal correlation between FS topology and properties (Tc, in this case). So, we have observed the importance of small FS’s for enhancing SC.

## Slide 91
Nodal nesting
Notes: And this general trend for IBS seems to be valid also for HTSC, taking into account that here the small FS’s formed as a result of AFM ordering. Such an ordering is observed for electron-doped side…

## Slide 92
VHS nesting
https://www.desmos.com/3d/2b44387285
Notes: While for holed doped side the situation is more complicated, relates to the nature of the PG… But the vast majority of evidence says that AFM ordering is present here too…

## Slide 93
SDW and superconductivity
A. A. Kordyuk Low Temp. Phys. (2018)
VHs nesting
Nodal nesting
Notes: And we expect that enhancement of Tc in cuprates has the same origin as in IBS.

## Slide 94
Superconducting qubits
15 mK
IBM Q
Notes: To illustrate the importance of Electronic Structure and FS for electronic applications, I go to SC quantum computers

## Slide 95
IBM 16-qubit processor
Nov 2021
IBM Quantum announced Eagle, a 127-qubit quantum processor based on the transmon superconducting qubit architecture
https://research.ibm.com/blog/eagle-quantum-processor-performance
Notes: While it is known that they need 10th thousands of SC qubits correlated, much less could be kept entangled now.

## Slide 96
Decoherence Is a Problem for Quantum Computing, but ...
https://blogs.scientificamerican.com/observations/decoherence-is-a-problem-for-quantum-computing-but/
The very thing quantum computers are battling is allowing the field of quantum measurements to blossom
Notes: And this decoherence problem seems to be a serious obstacle for future progress. One of the solutions is mentioned topological superconductivity, but another

## Slide 97
Modern standard: Aluminum technology!
TC / Δ
Al 1.8 K
0.3 meV
Nb 9.3 K
3 meV
Bi-2212 90 K
20 – -20 meV
BKFA 32 K
10, 3 & -10 meV
Notes: Could be essential increase of the frequency with which qubits communicate to each other. It depends on superconducting gap, that for Al, used in modern qubits, is 0.3 meV only. To try to increase it, we take the IBS that has gap 30 times larger

## Slide 98
Phys. Rev. Lett. 2018
Effect of the geometry of the Fermi surface on the Josephson effect between iron-pnictide and ordinary superconductor
Phys. Rev. B 2021
Notes: And managed to realize quite good JJ, but with extremely low IcRn (a key parameter that defines its frequency). This is a result of destructive interference of the tunneling current, and it could be another dead end, but we have found that a thin layer of Cu in between Nb and IBS enlarges the IcRn 40 times.

## Slide 99
The discovered effect
provides a new tool for phase-sensitive studies of superconducting condensate and
opens the way to intelligent engineering of new quantum devices in the reciprocal space
Phys. Rev. B 2021
The influence of the Fermi surface geometry on the Josephson effect
Notes: Explanation for this is tunneling filtering by an effective FC of Cu.
So, this effect
provides a new tool for phase-sensitive studies of superconducting condensate and
opens the way to intelligent engineering of new quantum devices in the reciprocal space

## Slide 100
The influence of the Fermi surface geometry on the Josephson effect
Notes: This slide for possible questions

## Slide 101
Synchrotron User Meetings

## Slide 102
Synchrotron Teams

## Slide 103
KAU
dS
Synchrotron 1990

## Slide 104
Leonid Rivkin
Eastern European Synchrotron Light Source in Ukraine?

## Slide 105
Leonid Rivkin
5th LEAPS Plenary Meeting, PSI, 26-28 October 2022
Eastern European Synchrotron Light Source in Ukraine?

## Slide 106
Marek Stankiewicz
Jakub Szlachetko
Ukrainian Beamline at SOLARIS
Light4Ukraine SOLARIS team
Artem Yakovliev
Anna Wach
Marcin Sikora
Marcin Zając
Michał Młynarczyk
Jarosław Wiechecki
Paweł Nowak
Piotr Piwowarczyk

## Slide 107: National Synchrotron Radiation Centre SOLARIS

## Slide 108
Light for Ukraine – synchrotron workshop at SOLARIS
23-24th February 2023
https://kau.org.ua/news/sci/937
https://indico.solaris.edu.pl/event/3/
Establishing the Ukrainian Synchrotron and Neutron Community
https://forms.gle/p3RhWX4s4jwwGnVf7

## Slide 109
Survey among Ukrainian researchers: nano/micro X-ray spectroscopy
Energy Range: 2.5-7(9) keV

## Slide 110
https://synchrotron.uj.edu.pl/en_GB/
SOLARIS storage ring Double-Bend Achromat (DBA) cells
The SOLARIS linear accelerator accelerates the electron beam produced in the electron gun to a speed of 99.99996 % of the speed of light (550 MeV). The beam is then injected into the storage ring (1.5 GeV).

## Slide 111
New Hall
Undulator
Photon source
Beamline
Experiment
LEAPS initiative
Luc Patthey, PSI
Danylo Babich, PSI

## Slide 112
Polish-Ukrainian beamline for X-ray spectroscopy/imaging applications with an in-vacuum undulator donated by the PSI SLS

## Slide 113
New Hall
Undulator
Photon source
Beamline
Experiment
LEAPS initiative
MAVKA
PSI team:
Luc Patthey
Danylo Babich
Marco Calvi
David Just
Rolf Follath
Leonid Rivkin
Glünkin Josua
With the strong support of Daniel Grolimund from SLS µXAS beamline

## Slide 114: Light for Ukraine Project Micro XAS/XRD Ukrainian beamline at SOLARIS: “MAVKA”
U19 from SLS
Toroidal Mirror and monochromator from µXAS SLS beamline
Total budget ~5.5 MCHF:
1 MCHF in-kind contribution from PSI
1.5 MCHF SERI/SNSF Grant

## Slide 115
L4U Workshop at SOLARIS
1-2 June 2025

## Slide 116: Summary timeline for L4U initiative
Oct 2023
Feasibility study
project and initiative of
Prof. Luc Patthey
from Paul Scherrer Institute, Switzerland.
Project Kick-off!
Oct 2022
LEAPS designates SOLARIS as the coordinator. Initiated by Prof. Leonid Rivkin.
Jun 2024
Approval of 1 MCHF SNF funding
Jun 2025
Finalizing the beamline conceptual design. Legal agreements between entities.
0.5 MCHF funding from SERI
Survey to investigate scientific potential and interest of Ukrainian society
Nov 2027
1st experiment
Employment of the project scientist (D. Babich) at PSI and project coordinator at SOLARIS (A. Levchuk).
CAD design of the beamline and ordering components
Transferring and commissioning components at SOLARIS.

## Slide 117
MAVKA Beamline for Ukraine’s Recovery
Ukraine must rebuild infrastructure, ensure environmental safety, restore healthcare capacity, and secure energy independence. The MAVKA beamline at SOLARIS (X-ray spectroscopy and imaging) offers a unique opportunity to align Ukrainian scientific expertise with urgent national recovery priorities.
Energy & Sustainability
Support solar cells, batteries, and doped ceramics for stable, decentralized energy.
Advance catalysis research for hydrogen, fuel cells, and pollution treatment.
Infrastructure & Environment
Develop durable superhard ceramics and steels for rebuilding.
Map and remediate toxic pollutants (heavy metals, radionuclides) in soil and water.
Health & Biomedicine
Apply spectroscopy and imaging to biopolymers, proteins, and membranes.
Strengthen drug discovery and diagnostics with synchrotron-enabled structural biology.
High-Tech & Innovation
Boost quantum materials research for electronics and sensors.
Cross-Cutting Benefits
Human capital: Training Ukrainian scientists in frontier synchrotron methods.
European integration: Positioning Ukraine within LEAPS/ESUO partnerships.

## Slide 118: East European Light Source (EELS) in Ukraine
A 4th generation synchrotron radiation source with 3 GeV energy
Capital expenditures: €250–400 million
Total building area: 43,000 m²
Site area: ~10 hectares
Construction timeline: 5–10 years
MAVKA also represents an important first step toward building

## Slide 119
Прикладна фізика та квантові технології
Теоретична та математична фізика
Фізичне матеріалознавство
E6
https://kau.edu.ua/education/kai-e6

## Slide 120
ExPhO 2025 — командну олімпіаду з фізичного експерименту. Перший тур відбудеться 13 квітня на базі Школи Базис, а другий тур -- 26 квітня на базі КАІ (в приміщенні Великого Ангару КАІ, де знаходяться багато цікавих літальних апаратів).
Олімпіада
ExPhO 2025 — це чудова нагода попрацювати в команді над рішенням цікавих експериментальних задач, навчитися колективно генерувати гіпотези розв'язків, швидко та якісно проводити експеримент для їх перевірки та захищати правильність своїх розв'язків у спілкуванні з журі.
https://kau.org.ua/news/sci/1384-expho-2025

## Slide 121
ExPhO в ангарі КАІ 2025